**Water-based rosin emulsion**

|  |  |
| --- | --- |
| **Description** | WPS-1005 is a product with rosin ester as raw material, light color, high softening point and excellent aging resistance. It is suitable for general-purpose pressure-sensitive adhesive system and can significantly improve the adhesive performance of adhesive products. |
| **Type** | Water-based rosin emulsion |
| **Key Features** | * Non-toxic, eco friendly * Using a unique surfactant, it significantly improves the initial tack, peel strength and tack of the adhesive after addition. * Small particle size, good mechanical stability, excellent flowability * Low surface tension, low foam, coating uniformity, no "fish eye" Online * Good compatibility: can significantly improve the adhesive products and achieve the best balance point |
| **Typical Properties** | |  |  |  |  |  |  |  | | --- | --- | --- | --- | --- | --- | --- | | **Model** | **WPS-1005A** | **WPS-1005B** | **WPS-1005C** | **WPS-1005D** | **WPS-1005E** | **WPS-1005F** | | **Solid Content** | **49-51%** | **49-51%** | **54-56%** | **49-51%** | **54-56%** | **54-56%** | | **PH Value** | **6-8** | **6-8** | **6-8** | **7-9** | **7-9** | **7-9** | | **Softening point** | **68-78** | **65-75** | **65-75** | **65-75** | **75-85** | **75-85** | | **Brookfield viscosity** | **600-1200** | **600-1200** | **100-600** | **600-1200** | **≤300** | **300-1000** | | **Particle size(Nm)** | **≤270nm** | **≤270nm** | **≤250nm** | **≤270nm** | **≤600nm** | **≤600nm** | |
| **APPLICATION** | * Water based paints * 叶面肥润湿剂2Waterbased adhesive * Natural and synthetic rubber emulsion * Interior and exterior building putty and other aspects |
| **Storage and Handling** | * Available in 200 kg/ barrel or 1000kg/barrel (IBC) * Store products in tightly closed original containers at 5-35℃ * Shelf life: 9-12 months from delivery date * According to non-dangerous goods transport |